## Slide 1: 3조
조장 | 유경환
곽대현 | 전제현
김규민 | 박재호
전민석 | 이준민

## Slide 2: Definition
Enclosure
Overlap
Spacing
Parallel length
한 도형의 외곽경계에서 다른 도형의 외곽까지의 거리
두 도형이 서로 겹쳐 있는 영역의 거리
한 도형이 다른 도형을 얼마나 감싸고 있는지를 나타내는 거리
두 도형의 서로 마주보는 가장자리가 겹쳐 있는 길이

## Slide 3: Layer colors
STI
METAL
POLY / Gate
CONTACTt
N+
P+
Nwell
OXIDE
Substrate
Thick OXIDE
IMD
VIA
ILD
Sillicide
SIPROT

## Slide 4: Nwell

## Slide 5
Substrate
Cadence Reproducing and vertical structure
Schematic in Design Rule Manual
Rule Name | Value | Description
NW.W.1 | 0.6um | Minimum Nwell width
0.6um
Nwell
✄
Nwell의 폭이 너무 좁으면 공정 오차로 인해
well이 정상적으로 형성되지 않을 수 있다.
0.6um
0.6um

## Slide 6
Substrate
Rule Name | Value | Description
NW.SP.1 | 0.6um | Minimum Nwell spacing to Nwell (same potential)
0.6um
Nwell
Nwell
✄
Nwell의 간격이 너무 좁으면 공정 오차로 인해
well이 서로 붙거나 형상이 변형돼
punch-through 현상이나 latch-up 현상이 일어날 수 있다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.6um

## Slide 7
Substrate
Rule Name | Value | Description
NW.SP.2 | 1.2um | Minimum Nwell spacing to Nwell (different potential)
1.2um
Nwell
Nwell
✄
서로 다른 전압이 인가되면 넓어지는 depletion 영역으로 인해 leakage path가 발생할 가능성이 더 커지므로
더 큰 최소 간격이 필요하다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
1.2um

## Slide 8
Rule Name | Value | Description
NW.SE.1 | 0.3um | Minimum Nwell spacing to N+ Active Area
0.3um
Nwell
STI
N+
STI
OXIDE
✄
두 영역이 너무 가까우면
latch up으로 인한 leakage path 현상이 발생할 수 있다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.3um

## Slide 9
Rule Name | Value | Description
NW.SE.2 | 0.3um | Minimum Nwell spacing to P+ Active Area
0.3um
Nwell
STI
STI
OXIDE
P+
✄
두 영역이 너무 가까우면
latch up으로 인한 leakage path 현상이 발생할 수 있다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.3um

## Slide 10
Rule Name | Value | Description
NW.SE.3 | 0.5um | Minimum Nwell spacing to N+ 2.5V Active Area
0.5um
Nwell
STI
N+
STI
Thick OXIDE
✄
더 큰 전압이 인가되어 더 큰 간격을 확보해야
leakage path 현상이 발생하지 않는다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.5um

## Slide 11
Rule Name | Value | Description
NW.SE.4 | 0.5um | Minimum Nwell spacing to P+ 2.5V Active Area
0.5um
Nwell
Thick OXIDE
P+
STI
STI
✄
더 큰 전압이 인가되어 더 큰 간격을 확보해야
leakage path 현상이 발생하지 않는다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.5um

## Slide 12
Rule Name | Value | Description
NW.E.1 | 0.12um | Minimum Nwell enclosure of N+ Active Area
0.12um
0.12um
Nwell
STI
STI
N+
OXIDE
✄
enclosure가 부족하면 공정 오차로 인해 active area가 Nwell 밖으로 벗어날 수 있어 안정된 active를 형성하기 위해 필요하다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.12um
0.12um
0.12um
0.12um

## Slide 13
Rule Name | Value | Description
NW.E.2 | 0.12um | Minimum Nwell spacing to P+ 2.5V Active Area
0.12um
0.12um
STI
STI
OXIDE
P+
✄
enclosure가 부족하면 공정 오차로 인해 active area가 Nwell 밖으로 벗어날 수 있어 안정된 active를 형성하기 위해 필요하다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.12um
0.12um
0.12um
0.12um

## Slide 14
Rule Name | Value | Description
NW.E.3 | 0.7um | Minimum Nwell enclosure of N+ 2.5V Active Area
0.7um
0.7um
STI
STI
Thick OXIDE
N+
✄
더 큰 전압이 인가되므로 보다 넓은 영역의 Nwell을 형성해야 안정된 active가 형성될 수 있다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.7um
0.7um
0.7um
0.7um

## Slide 15
Rule Name | Value | Description
NW.E.4 | 0.7um | Minimum Nwell enclosure of P+ 2.5V Active Area
0.7um
0.7um
STI
STI
Thick OXIDE
P+
✄
더 큰 전압이 인가되므로 보다 넓은 영역의 Nwell을 형성해야 안정된 active가 형성될 수 있다.
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.7um
0.7um
0.7um
0.7um

## Slide 16: Oxide

## Slide 17
Rule Name | Value | Description
OXIDE.W.1 | 0.1um | Minimum Active Area width
0.1um
Substrate
STI
N+
OXIDE
STI
빛의 회절 한계로 인해 패터닝 가능한 최소 실리콘 영역, oxide를 균일하게 채워 넣을 수 있는 최소 물리적 공간을 의미
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.1um

## Slide 18
Rule Name | Value | Description
OXIDE.W.2.1.1 | 0.12um | Minimum 1.2V N-channel gate width
0.12um
Substrate
STI
STI
폭이 너무 좁아지면 문턱 전압 변동성이 커지고 누설 전류가 증가하므로 이를 방지하고 안정적인 전류를 확보하기 위한 최소 채널 폭
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.12um

## Slide 19
Rule Name | Value | Description
OXIDE.W.3 | 0.13um | Minimum Active Area bent 45 degrees width
0.13um
Substrate
STI
STI
포토리소그래피 공정에서 45도 사선 마스크 패턴은 격자배치 및 노광 시 감광액이 잘려 나가는
현상이 발생해서 0.13µm보다 두꺼운 설계 필요
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.13um

## Slide 20
Rule Name | Value | Description
OXIDE.SP.1 | 0.15um | Minimum N+ Active Area to N+ Active Area spacing
0.15um
Substrate
OXIDE
N+
OXIDE
N+
STI
STI
두 Active 패턴 사이의 거리가 너무 가까우면
STI 식각 후 Oxide를 채워 넣을 때
내부에 빈 공간이 생겨 short가 발생할 수 있음
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.15um

## Slide 21
Rule Name | Value | Description
OXIDE.SP.2 | 0.15um | Minimum P+ Active Area to P+ Active Area spacing
0.15um
Substrate
Nwell
P+
OXIDE
P+
OXIDE
STI
STI
두 Active 패턴 사이의 거리가 너무 가까우면
STI 식각 후 Oxide를 채워 넣을 때
내부에 빈 공간이 생겨 short가 발생할 수 있음
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 22
Rule Name | Value | Description
OXIDE.SP.3 | 0.15um | Minimum N+ Active Area to P+ Active Area spacing
0.18um
Substrate
Nwell
OXIDE
P+
OXIDE
STI
STI
N+
두 Active 패턴 사이의 거리가 너무 가까우면
STI 식각 후 Oxide를 채워 넣을 때
내부에 빈 공간이 생겨 short가 발생할 수 있음
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.18um

## Slide 23
Rule Name | Value | Description
OXIDE.SP.4 | 0.18um | Minimum Active Area bent 45 degrees to Active Area spacing
0.18um
Substrate
STI
STI
45도 기울어진 패턴이 맞닿는 부분은
빛의 간섭 현상으로 인해
마스크 패턴이 쉽게 뭉개지거나 연결될 위험이 큼
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.18um

## Slide 24
Rule Name | Value | Description
OXIDE.SE.1 | 0.28um | Minimum Active Area to Thick Active Area spacing
0.28um
Substrate
STI
Thick OXIDE
N+
얇은 oxide와 두꺼운 oxide 영역을 구분하기 위해 'Dual Oxide Mask'를 사용하는
추가 Etch 공정이 들어가며 두 영역 간의
마스크 정렬 오차 안정성을 보장하기 위해
일반 간격보다 훨씬 넓은 마진(0.28um)이 필요
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.28um

## Slide 25
Rule Name | Value | Description
OXIDE.A.1 | 0.06um | Minimum area for Active Area
0.3um
Substrate
STI
N+
OXIDE
STI
Active 면적이 너무 작은 형태로 존재하면
CMP 공정 중에 연마 패드의 강한 마찰력을
견디지 못하고 패턴이 탈락되어 웨이퍼 오염을 유발
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.3um

## Slide 26
Rule Name | Value | Description
OXIDE.EA.1 | 0.1um | Minimum Active Area enclosed area ("donut" hole surrounded by Active Area)
0.5um
Substrate
STI
STI
Active 영역이 도넛 형태로 둘러싸고 있는 내부 구멍이 너무 작으면 식각 액체나 세정 케미컬의
표면장력 때문에 액체가 갇히므로
이로 인해 미식각 영역이 남는 결함이 발생
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.5um
0.2um

## Slide 27
ILD
N+
OXIDE
Rule Name | Value | Description
OXIDE.L.1 | 22um | Maximum Oxide length between two contacts when the Oxide width is <= 0.18um.
Substrate
STI
METAL
22um
0.18 µm 이하의 얇은 Active 선이
컨택(Contact) 없이 너무 길게 늘어서면
심각한 전압 강화(IR Drop) 및 RC delay가 발생
Contact ~ Contact 사이 거리 22um
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
22um

## Slide 28
ILD
Rule Name | Value | Description
OXIDE.L.2 | 11um | Maximum Oxide length between one contact and the end of the Oxide line when the Oxide width is <= 0.18um
N+
OXIDE
Substrate
STI
METAL
11um
0.18 µm 이하의 얇은 Active 선이
컨택(Contact) 없이 너무 길게 늘어서면
심각한 전압 강화(IR Drop) 및 RC delay가 발생
Contact ~ Oxide 끝 사이 거리 11um
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
11um

## Slide 29: POLY

## Slide 30
Substrate
Rule Name | Value | Description
POLY.W.1 | 0.1um | Minimum 1.2V N-channel gate length
✄
0.1um
OXIDE
STI
N+
STI
N+
“Short Channel Effect와 누설전류 증가를 방지하기 위해 NMOS의 최소 Gate Length를 제한”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.1um

## Slide 31
Substrate
Nwell
Rule Name | Value | Description
POLY.W.2 | 0.1um | Minimum 1.2V P-channel gate length
0.1um
✄
OXIDE
STI
STI
P+
P+
“PMOS의 전기적 특성과 신뢰성을 유지하기 위해 최소 Gate Length를 제한”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.1um

## Slide 32
Rule Name | Value | Description
POLY.W.3 | 0.28um | Minimum 2.5V N-channel gate length
0.28um
✄
Substrate
STI
N+
STI
N+
Thick OXIDE
“고전압 동작 시 Hot Carrier Injection과 Gate Oxide 열화를
방지하기 위해 최소 Gate Length를 제한”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.28um

## Slide 33
Rule Name | Value | Description
POLY.W.4 | 0.28um | Minimum 2.5V P-channel gate length
✄
0.28um
Substrate
Nwell
STI
STI
P+
P+
Thick OXIDE
“고전압 동작 시 Hot Carrier Injection과 Gate Oxide 열화를
방지하기 위해 최소 Gate Length를 제한”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.28um

## Slide 34
Rule Name | Value | Description
POLY.W.5 | 0.1um | Minimum Poly interconnect width
q
0.1um
“Poly 배선의 단선과 저항 증가를 방지하기 위해 최소 Poly 폭을 규정”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.1um

## Slide 35
Rule Name | Value | Description
POLY.SP.1 | 0.6um | Minimum Poly resistor space
0.6um
Substrate
STI
“Poly 저항의 저항값 오차와 공정 간섭을 줄이기 위해 최소 간격을 확보”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.6um

## Slide 36
Rule Name | Value | Description
POLY.SP.2 | 0.12um | Minimum gate space
✄
0.12um
Substrate
STI
N+
STI
N+
OXIDE
“인접한 Gate의 브리징과 기생 capacitor 증가를 방지하기 위해 최소 Gate 간격을 유지.”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.12um

## Slide 37
Substrate
Rule Name | Value | Description
POLY.SP.3 | 0.12um | Minimum Poly interconnect space
0.12um
STI
“Poly 배선 간 브리징과 signal 간섭을 방지하기 위해 최소 배선 간격을 유지”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.12um

## Slide 38
Rule Name | Value | Description
POLY.E.1 | 0.18um | Minimum N-channel gate extension beyond Active Area
✄
0.18um
Substrate
OXIDE
STI
STI
“Gate Contact 배치 공간을 확보하고 Overlay 오차를 보상하기 위해 Gate Poly를 Active 밖으로 충분히 연장”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.18um

## Slide 39
Substrate
Nwell
Rule Name | Value | Description
POLY.E.2 | 0.18um | Minimum P-channel gate extension beyond Active Area
0.18um
✄
OXIDE
STI
STI
“Gate Contact 배치 공간을 확보하고 Overlay 오차를 보상하기 위해 Gate Poly를 Active 밖으로 충분히 연장”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.18um

## Slide 40
Rule Name | Value | Description
POLY.E.3 | 0.2um | Minimum Active Area (source/drain) to gate enclosure
✄
0.2um
Substrate
OXIDE
STI
N+
STI
N+
“Source/Drain과 Gate의 정렬 오차를 보상하고 안정적인 채널 형성을 위해 충분한 Active Enclosure를 확보”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.2um

## Slide 41
Substrate
Rule Name | Value | Description
POLY.SE.1_2 | 0.1um | Minimum Poly interconnect to unrelated/related Active Area space
0.1um
✄
STI
STI
N+
OXIDE
POLY / Gate
“의도하지 않은 MOS 채널 형성과 단락을 방지하기 위해 Poly와 Active 사이의 최소 간격을 유지”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.1um

## Slide 42
Rule Name | Value | Description
POLY.W.6 | 0.18um | Minimum bent Poly width
Substrate
STI
0.18um
POLY / Gate
“Corner Rounding으로 인한 폭 감소와 단선을 방지하기 위해 Bent Poly의 최소 폭을 규정”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.18um

## Slide 43
POLY / Gate
Substrate
STI
0.18um
POLY / Gate
0.22um
0.18um
“Bent Poly에서 발생하는 패턴 왜곡과 브리징을 방지하기 위해 최소 간격을 적용”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.22um
Rule Name | Value | Description
POLY.SP.4 | 0.22um | Minimum bent Poly space

## Slide 44
Substrate
✄
Bends==0
OXIDE
STI
N+
STI
N+
“균일한 채널 형성과 안정적인 소자 특성을 위해 Bent Gate를 금지. 직선 구조만 사용”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Rule Name | Value | Description
POLY.X.1 | --- | Bent gate is not allowed

## Slide 45
Rule Name | Value | Description
POLY.X.2 | --- | Bent Poly resistor is not allowed
Substrate
✄
Bends==0
STI
“Current Crowding과 저항값 오차를 방지하기 위해 Bent Poly Resistor를 금지”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 46
Rule Name | Value | Description
POLY.D.1 | 50% | Maximum Poly density across full chip
“Poly Density Ratio를 제한하여 CMP와 식각 공정의 균일성을 확보”
Schematic in Design Rule Manual

## Slide 47
Rule Name | Value | Description
POLY.SE.3 | 25.0 | Minimum Poly segment length (width < 0.14) between two contacts
“좁고 긴 Poly의 높은 저항과 IR Drop을 방지하기 위해 최대 Poly Segment Length를 제한”
Schematic in Design Rule Manual

## Slide 48
Rule Name | Value | Description
POLY.A.1 | 0.1 | Minimum area for Poly interconnect
“공정에서 안정적으로 패턴을 형성하기 위해 Poly의 최소 면적을 확보”
Schematic in Design Rule Manual

## Slide 49: Implant

## Slide 50
Rule Name | Value | Description
NIMP.W.1 | 0.24um | Minimum N+ Implant width
0.24
STI
도핑 균일성과 Source/Drain 특성 확보를 위한
최소 N+ Implant width
0.24
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 51
Rule Name | Value | Description
NIMP.SP.1 | 0.24um | Minimum N+ Implant space
0.24
STI
N+
N+
도핑 영역 간 간섭 및 Short 방지를 위한
최소 Implant space
0.24
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 52
Rule Name | Value | Description
NIMP.E.1 | 0.14um | Minimum N+ Implant to Active Area enclosure
STI
STI
N+
OXIDE
Active Area의 안정적인 도핑을 위한
최소 Enclosure
0.14
0.14
0.14
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 53
Rule Name | Value | Description
NIMP.O.1 | 0.16um | Minimum N+ Implant to Active Area overlap
STI
STI
OXIDE
N+
P+
0.16
공정 오차를 고려한 Active Area와 Implant의
최소 Overlap
0.16
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 54
Nwell
Rule Name | Value | Description
NIMP.SE.1 | 0.16um | Minimum N+ Implant to P+ Active (inside Nwell) Area spacing
STI
STI
P+
OXIDE
Nwell 내부 N+/P+ 간 누설전류 방지를 위한
최소 space
0.16
0.16
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 55
Nwell
Rule Name | Value | Description
NIMP.E.2 | 0.02um | Minimum N+ Implant to Active Area (Nwell tie) enclosure
STI
OXIDE
N+
STI
Nwell tie의 안정적인 전위 유지를 위한
최소 enclosure
0.02
0.02
0.02
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 56
Rule Name | Value | Description
NIMP.E.3 | 0.18um | Minimum N+ Implant to gate side enclosure
STI
STI
OXIDE
N+
N+
Gate 주변 Source/Drain 형성 보장을 위한
최소 enclosure
0.18
0.18
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 57
Rule Name | Value | Description
NIMP.SE.2 | 0.02um | Minimum N+ Implant to P+ Active Area (substrate tie) spacing
STI
STI
P+
OXIDE
Substrate Tie의 안정적인 기판 전위 유지를 위한 최소 space
0.02
0.02
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 58
Rule Name | Value | Description
NIMP.E.4 | 0.18um | Minimum N+ to gate (endcap) enclosure
STI
STI
OXIDE
Gate Endcap에서 안정적인 Source/Drain 형성을 위한
최소 Enclosure
0.18
0.18
0.18
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 59
Rule Name | Value | Description
NIMP.SE.3 | 0.18um | Minimum N+ Implant to P+ gate side (butted Implant) spacing
Nwell
STI
OXIDE
N+
STI
P+
N+/P+ 도핑 간 간섭 방지를 위한 최소 space
0.18
0.18
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 60
Rule Name | Value | Description
NIMP.A.1 | 0.15um | Minimum area for N+ Implant
STI
공정 재현성 확보를 위한 최소 Implant area
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 61
Rule Name | Value | Description
NIMP.EA.1 | 0.16um | Minimum N+ Implant ring enclosed area ("donut" hole surrounded by N+ Implant)
STI
Donut Implant의 제조 가능성 확보를 위한
최소 Enclosed Area
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 62
Rule Name | Value | Description
NIMP.X.1 | --- | N+ Implant is NOT allowed over P+ Implant
정상적인 PN Junction 형성을 위한
N+/P+ Implant 중첩 금지
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 63: Contact

## Slide 64
✄
Rule Name | Value | Description
CONT.W.1 | 0.12um | Minimun Contact to Contact width/length
0.12um
0.12um
0.12um
Substrate
Silicide
OXIDE
CONTACTt
N+
공정 안정성 및 Contact 저항 감소를 위한
최소 Contact 크기
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Silicide

## Slide 65
Rule Name | Value | Description
CONT.SP.1 | 0.14um | Minimun Contact to Contact spacing
0.12um
0.14um
✄
Substrate
CONTACT
N+
Silicide
Silicide
OXIDE
CONTACT
공정 안정성 및 Short 방지를 위한 최소 Contact 간격
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Silicide
Silicide

## Slide 66
Rule Name | Value | Description
CONT.SE.1 | 0.10um | Minimum Contact on Active Area to gate spacing
✄
0.10um
0.10um
Substrate
Silicide
OXIDE
CONTACTt
ILD
METAL 1
N+
Gate 손상·Short 방지를 위한
최소 Contact-Gate 간격
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Silicide
ILD

## Slide 67
ILD
ILD
Rule Name | Value | Description
CONT.SE.3 | 0.12um | Minimum gate Contact to Active Area spacing
0.12um
0.12um
✄
Substrate
STI
POLY / Gate
CONTACTt
Gate-Active Short 방지를 위한 최소 Gate Contact 간격
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 68
Rule Name | Value | Description
CONT.E.1 | 0.06um | Minimum Active Area to Contact enclosure
0.06um
0.06um
✄
0.06um
Substrate
Sillicide
OXIDE
CONTACTt
ILD
METAL 1
N+
STI
안정적인 Contact 형성 및 Contact 저항 감소를 위한 Active Area Enclosure 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Sillicide
ILD

## Slide 69
Rule Name | Value | Description
CONT.E.2 | 0.04um | Minimum Poly to Contact enclosure
0.04um
0.04um
0.04um
✄
Substrate
STI
POLY
ILD
CONTACTt
안정적인 Gate Contact 형성 및 Contact 저항
감소를 위한 Poly Enclosure 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 70
Rule Name | Value | Description
CONT.E.3 | 0.06um | Minimum Poly to Contact enclosure on at least two opposite sides (end of line)
0.06um
0.06um
✄
Substrate
STI
POLY / Gate
ILD
CONTACT
안정적인 Contact 형성 및 Open 방지를 위한 Poly Enclosure 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 71
Substrate
Rule Name | Value | Description
CONT.E.4 | 0.06um | Minimum N+/P+ Implant on Active Area to Contact enclosure
0.06um
0.06um
0.06um
0.06um
✄
P+
CONTACT
Sillicide
OXIDE
OXIDE
0.06um
Substrate
CONTACT
Sillicide
OXIDE
OXIDE
0.06um
N+
안정적인 Ohmic Contact 형성 및 Contact 저항 감소를 위한 Implant Enclosure 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Sillicide
Sillicide

## Slide 72
Rule Name | Value | Description
CONT.SE.5 | 0.24um | Minimum Poly Contact to non-salacided Poly resistor or Active Contact to non-salacided Active resistor spacing
0.24um
0.24um
✄
Substrate
STI
CONTACTt
POLY / Gate
Silicide
저항 특성 유지 및 Salicide 침범 방지를 위한 최소 Contact-Resistor 간격 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Silicide

## Slide 73: Salicide

## Slide 74
Rule Name | Value | Description
SIPROT.W.1 | 0.44um | Minimum Salicide Block width
얇으면 공정 오차 ↑
0.44
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 75
Rule Name | Value | Description
SIPROT.SP.1 | 0.44um | Minimum Salicide Block space
가까우면 공정 오차 ↑
0.44
0.44
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 76
Rule Name | Value | Description
SIPROT.SE.1 | 0.24um | Minimum Salicide Block to Contact spacing
Contact 근처에는 저항,신뢰성 문제가 큼
0.24
contact
silicide
poly
STI
P-Substrate
0.24
✄
SIPROT
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 77
ILD
Rule Name | Value | Description
SIPROT.SE.2 | 0.24um | Minimum Salicide Block to Unrelated Active Area spacing
0.24
silicide
STI
P-Substrate
Active 영역의 edge에서 도핑과 실리사이드 형성이 불안정해지는 것을 방지
N+
0.24
✄
SIPROT
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 78
ILD
Rule Name | Value | Description
SIPROT.SE.3 | 0.44um | Minimum Salicide Block to gate spacing
silicide
P-Substrate
N+
Gate 위 silicide가 불균일해지는 것을 방지
OXIDE
silicide
silicide
poly
N+
STI
STI
0.44
0.44
✄
SIPROT
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 79
Rule Name | Value | Description
SIPROT.E.1 | 0.25um | Minimum Salicide Block to Active Area enclosure
P-Substrate
Silicide를 확실하게 막기 위해서
N+
STI
0.25
0.25
✄
SIPROT
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 80
Rule Name | Value | Description
SIPROT.E.2 | 0.24um | Minimum Active Area to Salicide Block enclosure
P-Substrate
Active edge를 확실히 덮기 위해서
N+
STI
0.24
silicide
0.24
SIPROT
✄
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 81
ILD
Rule Name | Value | Description
SIPROT.E.3 | 0.28um | Minimum Salicide Block to Poly (on field) enclosure
P-Substrate
STI 위 Poly는 silicide 대상이 아니므로충분히 덮어 오동작 방지
STI
poly
STI
✄
SIPROT
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.28
0.28
0.28
0.28

## Slide 82
Rule Name | Value | Description
SIPROT.A.1 | 1.2um | Minimum Salicide Block area
마스크/공정 오차를 위해
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 83
Rule Name | Value | Description
SIPROT.EA.1 | 1.2um | Minimum Salicide Block enclosed area ("donut" hole surrounded by Salicide Block)
공정 신뢰성을 확보하기 위해
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 84
Rule Name | Value | Description
SIPROT.SE.4 | 0.35um | Minimum Salicide Block to Poly (on field) spacing
P-Substrate
STI 위 Poly 근처에 silicide가 생겨 일어날 저항 문제 방지
STI
silicide
poly
0.35
SIPROT
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
0.35

## Slide 85: Metal

## Slide 86
Rule Name | Value | Description
METAL1.W.1 | 0.12um | Minimum Metal 1 width
0.12um
✄
0.12um
Substrate
Silicide
OXIDE
CONTACTt
ILD
METAL 1
N+
공정 안정성 및 배선 신뢰성 확보를 위한 최소 Metal1 폭 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Silicide
ILD

## Slide 87
Rule Name | Value | Description
METAL1.W.2 | 12um | Maximum Metal 1 width
12um
12um
✄
Substrate
ILD
STI
METAL
공정 안정성 및 배선 신뢰성 확보를 위한
최대 Metal1 폭 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 88
Rule Name | Value | Description
METAL1.SP.1.1 | 0.12um | Minimum Metal 1 to Metal 1 spacing
0.12um
0.12um
✄
Substrate
STI
ILD
METAL
METAL
0.12um
0.12um
공정 안정성 및 배선 간 Short 방지를 위한 최소 Metal1 간격 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 89
Rule Name | Value | Description
METAL1.SP.1.2 | 0.18um | Minimum Metal 1 to Metal 1 spacing
If one metal width > 0.18 and parallel length > 0.56
0.18um
0.18um
0.18um
✄
Substrate
STI
ILD
METAL
METAL
0.56um
0.18um
0.18um
공정 안정성 및 Crosstalk 감소를 위한 최소 Metal1 간격 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 90
Rule Name | Value | Description
METAL1.SP.1.3 | 0.50um | Minimum Metal 1 to Metal 1 spacing
If one metal width > 1.5 and parallel length > 1.5
0.50um
0.50um
✄
Substrate
STI
ILD
METAL
METAL
0.50um
1.5um
폭 증가 → Bridge 위험 증가
평행 길이 증가 → Short 위험 증가
평행 길이 증가 → Crosstalk 증가
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 91
Rule Name | Value | Description
METAL1.SP.1.4 | 0.90um | Minimum Metal 1 to Metal 1 spacing
If one metal width > 3.0 and parallel length > 3.0
0.90um
0.9um
0.9um
✄
STI
Substrate
ILD
METAL
METAL
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 92
Rule Name | Value | Description
METAL1.SP.1.5 | 1.50um | Minimum Metal 1 to Metal 1 spacing
If one metal width > 4.5 and parallel length > 4.5
1.50um
1.5um
1.5um
✄
Substrate
STI
ILD
METAL
METAL
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 93
Rule Name | Value | Description
METAL1.SP.1.6 | 2.50um | Minimum Metal 1 to Metal 1 spacing
If one metal width > 7.5 and parallel length > 7.5
2.50um
2.5um
2.5um
✄
Substrate
STI
ILD
METAL
METAL
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 94
Substrate
Rule Name | Value | Description
METAL1.E.1 | 0.00um | Minimun Metal 1 to Contact enclosure
0.12um
0.12um
0.12um
STI
STI
Silicide
OXIDE
OXIDE
CONTACTt
ILD
ILD
METAL 1
N+
✄
안정적인 Contact 형성 및 Open 방지를 위한 Metal1 Enclosure 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Silicide
ILD
ILD

## Slide 95
Rule Name | Value | Description
METAL.E.2 | 0.06um | Minimun Metal 1 to Contact enclosure on two opposite sides of the Contact
0.06um
✄
0.06um
Substrate
Silicide
OXIDE
OXIDE
CONTACTt
ILD
ILD
METAL 1
N+
STI
정렬 오차 보정
안정적인 전류 전달 확보
Open 및 contact 저항 증가 방지
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Silicide
ILD
ILD

## Slide 96
Rule Name | Value | Description
METAL1.L.1 | 0.18um | Minimun bent Metal1(45 degree angle) length
0.18um
✄
0.18um
Substrate
ILD
METAL 1
STI
45° 패턴 형성 안정성 확보
식각 공정 안정성 확보
Open및 배선 불량 방지
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 97
Rule Name | Value | Description
METAL1.SP.2 | 0.16um | Minimun bent Metal1(45 degree angle) space
0.16um
✄
Substrate
ILD
STI
0.16um
공정 안정성 및 Short 방지를 위한 최소 45° Metal1 간격 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 98
Rule Name | Value | Description
METAL1.W.3 | 0.14um | Minimun bent Metal1(45 degree angle) width
0.14um
✄
0.14um
Substrate
ILD
STI
공정 안정성 및 배선 신뢰성 확보를 위한 최소 45° Metal1 폭 규정
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 99
Rule Name | Value | Description
METAL1.A.1 | --- | Minimum bent Metal1 area
✄
Substrate
ILD
STI
공정 안정성 및 배선 신뢰성 확보를 위한 최소 Metal1 면적 규정
0.59um
0.12um
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD

## Slide 100
Density Window Stepping(60um increments)
Rule Name | Value | Description
METAL1.D.1 | 65%~20% | Metal 1 Density range over any 120um x 120um area (checked by stepping in 60um increments)
Base window 120um x 120um
60um
60um
CMP 공정 안정성 확보
공정 균일성 확보
배선 신뢰성 확보
Cadence Reproducing and vertical structure

## Slide 101
Density Window Stepping(300um increments)
Rule Name | Value | Description
METAL1.D.2 | <60% | Metal 1 Density range over any 600um x 600um area (checked by stepping in 300um increments)
Base window 600um x 600um
300um
300um
대면적 CMP 안정성 확보
공정 균일성 확보
배선 신뢰성 확보
Cadence Reproducing and vertical structure

## Slide 102: Via

## Slide 103
Substrate
Rule Name | Value | Description
VIAk.W.1 | 0.14um | Minimum and Maximum Via k width
0.14um
STI
Via7, Via8 Minimum and Maximum width = 0.36um
ILD
“Via의 폭을 적절한 범위로 제한하여 금속층 간 안정적인 연결과 공정 신뢰성을 확보”
metal1
IMD
IMD
metal2
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
ILD
IMD
IMD

## Slide 104
Rule Name | Value | Description
VIAk.SP.1 | 0.15um | Minimum Via k to Via k spacing
Via7, Via8 spacing = 0.36um
“인접한 Via 사이의 최소 간격을 확보하여 브리징을 방지하고 공정 수율 및 전기적 신뢰성을 확보”
0.15um
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Substrate
STI
ILD
metal1
IMD
IMD
metal2
IMD

## Slide 105
Rule Name | Value | Description
VIAk.SP.2 | 0.20um | Minimum Via k to Via k spacing when the Via ks are in a 3x3 or larger array (minimum dimension on one side of array is 3). Via ks spaced less than 0.21um should be considered for array spacing check.
0.2um
“3×3 이상의 Via Array에서는 Via가 밀집되면서 식각 및 금속 매립 공정의 균일성이 저하되어 Void, 브리징 등의 결함이 발생할 수 있으므로, 공정 신뢰성과 수율을 확보하기 위해 더 큰 최소 간격을 적용”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Substrate
STI
ILD
metal1
IMD
IMD
metal2
IMD
IMD

## Slide 106
Rule Name | Value | Description
VIAk.E.1 | 0.005um | Minimum Metal k to Via k enclosure
0.005um
“Via를 네 방향에서 충분히 감싸 안정적인 금속층 연결과 공정 신뢰성을 확보” (각 면당 최소 0.005um 이상 권장)
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Substrate
STI
IMD
METAL1

## Slide 107
0.06um
Rule Name | Value | Description
VIAk.E.2 | 0.06um | Minimum Metal k to Via k enclosure on at least two opposite sides of Via k
“Via의 마주보는 두 방향에서 충분한 Enclosure를 확보하여 Overlay 오차에도 안정적인 접촉을 보장”
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure
Substrate
STI
IMD
METAL1
IMD
ILD

## Slide 108
넓은 Metal 연결부의 전류 분산과 신뢰성 확보를 위해 최소 개수의 Via를 배치
≤ 0.3 um
ILD
METAL 2
IMD
METAL 1
STI
> 0.4 um
Rule Name | Value | Description
VIAk.X.1 | --- | Minimum of two Via k with spacing <= 0.30um or four Via k with spacing <= 0.60um are required when connecting Metal k and Metal k+1 when one of the Metals has a width > 0.40um at the connection point
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 109
더 넓은 Metal에서는 더 큰 전류를 고려하여
더 많은 Via 개수를 요구
≤ 0.3 um
> 0.4 um
ILD
METAL 2
IMD
METAL 1
STI
Rule Name | Value | Description
VIAk.X.2 | --- | Minimum of four Via k with spacing <= 0.30um or nine Via k with spacing <= 0.60um are required when connecting Metal k and Metal k+1 when one of the Metals has a width > 1.0um at the connection point
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 110
단일 Via Stack은 신뢰성 확보를 위해
최대 4층까지만 허용
ILD
IMD
STI
IMD
IMD
IMD
METAL 2
METAL 1
Rule Name | Value | Description
VIAk.X.3 | --- | Vias 1 through 6 may be consecutively stacked up to four high when only one Via is connecting two Metal layers for any level of the stack
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 111
각 층에 2개 이상의 Via를 사용하면
전류 분산을 통해 4층 이상의 Via Stack을 허용
ILD
IMD
STI
IMD
IMD
IMD
METAL 2
METAL 1
( • • • )
IMD
( • • • )
Rule Name | Value | Description
VIAk.X.4 | --- | Vias 1 through 6 may be consecutively stacked up more than four high when at least two Vias are connecting two Metal layers for all levels of the stack
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 112: Latch up

## Slide 113
Rule Name | Value | Description
LATCHUP.1 | 25um | The maximum distance from any point in a P+ source/drain Active Area to the nearest Nwell pick-up in the same Nwell.
P-Substrate
25
Nwell
N+
P+
P+
oxide
poly
기생 BJT가 켜져서 latch-up이 발생하는 걸 막기 위해
STI
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 114
Rule Name | Value | Description
LATCHUP.2 | 25um | The maximum distance from any point in an N+ source/drain Active Area to the nearest Psub pick-up in the same Psub
P-Substrate
25
N+
N+
oxide
poly
P+
기생 BJT가 켜져서 latch-up이 발생하는 걸 막기 위해
STI
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 115: Antenna

## Slide 116
Rule Name | Value | Description
ANT.1 | 275um | Maximum ratio of Poly area to the gate area the Poly is connected to
공정 중 poly에 축적된 전하로 인해 gate oxide가
손상되는 것을 방지하기 위함이다.
✄
Gate area
Poly on
field area
Substrate
STI
STI
POLY
OXIDE
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 117
Rule Name | Value | Description
ANT.2 | 550um | Maximum ratio of Poly sidewall area to the gate area the Poly is connected to
Poly 측면에 축적되는 전하로 인해 gate oxide가 손상되지 않게
하기 위함이다.
✄
Gate area
Substrate
STI
STI
POLY
OXIDE
Poly on field perimeter
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 118
ILD
Rule Name | Value | Description
ANT.3 | 15 | Maximum ratio of Poly Contact area to the gate area the Contact is connected with
Contact을 통해 전달되는 과도한 전하로부터 gate oxide를
보호하기 위함이다.
Substrate
STI
STI
POLY
OXIDE
✄
Gate area
Cont antenna area
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 119
ILD
Rule Name | Value | Description
ANT.4 | 475 | Maximum ratio of single level Metal x (x = 1, 2, 3, 4, 5, 6, 7, 8, 9) area to the (gate area + 2*Diff area)
공정 중 metal에 축적되는 전하로 부터 gate를 보호하기 위함이다.
Substrate
STI
STI
OXIDE
✄
Gate area
Diff diode area
Metal1 conn area
N+
METAL 1
STI
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 120
ILD
Rule Name | Value | Description
ANT.5 | 25 | Maximum ratio of single level Via x (x = 1, 2, 3, 4, 5, 6, 7, 8) area to the (gate area + 2*Diff area)
공정 중 via를 통해 축적되는 전하로 부터 gate를 보호하기 위함이다.
Substrate
STI
STI
OXIDE
Gate area
Diff diode area
Via x area
N+
METAL 1
IMD
✄
STI
METAL 2
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure

## Slide 121
Rule Name | Value | Description
ANT.6 | 1200 | Maximum ratio of cummulative multi level Metal areas to the (gate area + 2*Diff area)
공정 중 여러 metal 층에 축적된 전하가 gate oxide를 손상시키는
것을 방지하기 위함이다.
Gate area
Diff diode area
Metal1 conn area
Metal2 conn area
ILD
Substrate
STI
STI
OXIDE
N+
METAL 1
IMD
✄
STI
METAL 2
Schematic in Design Rule Manual
Cadence Reproducing and vertical structure