## Slide 1: 3조
조장 | 유경환
곽대현 | 전제현
김규민 | 박재호
전민석 | 이준민

## Slide 2: Definition
Enclosure
Overlap
Spacing
Parallel length
한 도형의 외곽경계에서 다른 도형의 외곽까지의 거리
한 도형이 다른 도형을 얼마나 감싸고 있는지를 나타내는 거리
두 도형이 서로 겹쳐 있는 영역의 거리
두 도형의 서로 마주보는 가장자리가 겹쳐 있는 길이

## Slide 3: Layer colors
STI
METAL
POLY / Gate
CONTACTt
N+
P+
Nwell
OXIDE
Substrate
Thick OXIDE
IMD
VIA
ILD
Sillicide

## Slide 4
Design Rule 이면의 공통 배경 : 공정상의 한계
1
LITHOGRAPHY 한계
노광 해상도의 한계
너무 작은 패턴은 노광 과정에서 의도한 모양대로 만들어지지 않음
관련: 대부분의 최소 Width / Length 규정
2
ETCHING 한계
식각 공정의 한계
좁고 깊은 Hole·Line은 식각이 끝까지 진행되지 않거나 형상이 변형됨
관련: Width, Enclosure 규정
3
SHORT CIRCUIT 방지
인접 패턴 간 단락 방지
공정 오차로 인접한 두 패턴이 붙어(Bridge) 전기적으로 단락되는 것을 방지
관련: 대부분의 Spacing 규정
4
OVERLAY 정렬 오차
마스크 정렬 오차 보정
포토마스크 정렬 시 발생하는 오차를 흡수할 여유 마진 확보
관련: 대부분의 Enclosure 규정

## Slide 5: Why METAL and CONTACT?
Heterojunction : An interface formed between two dissimilar semiconductor materials with unequal band gaps.
Interface physics — not bulk physics — is what makes heterojunctions interesting
Type-Ⅰ Heterojunction (schematic)
E
Ec
Ec
Ev
Ev
ΔEc
ΔEv
Semiconductor A
(narrow gap)
Semiconductor B
(wide gap)
* 이상적인 straddling-gap (Type-Ⅰ) 배치를 나타낸 개념도

## Slide 6: To Interface Physics
Heterogeneous interfaces host a range of fascinating physical phenomena that don't emerge in either bulk material alone.
Heterojunction
A
B
ΔEc, ΔEv
전자 친화도 / work function 차이 → band offset 결정
Metal – Semiconductor Junction
EF
φB
M
S
Metal / Semiconductor work function 차이 → Schottky barrier 결정 (Schottky–Mott rule)
Heterogeneous interfaces host physics found nowhere else — this is why I chose to explore how these effects shape Contact / Metal1 Design Rule.

## Slide 7: Contact

## Slide 8
Cadence Reproducing and vertical structure
Cadence
Schematic in Design Rule Manual
Rule Name | Value | Description
CONT.SE.1 | 0.10um | Minimum Contact on Active Area to gate spacing
✄
0.10um
0.10um
Substrate
Silicide
OXIDE
CONTACTt
ILD
METAL 1
N+
Gate 손상·Short 방지를 위한 최소 Contact-Gate 간격

## Slide 9
ILD
Cadence Reproducing and vertical structure
Cadence
Schematic in Design Rule Manual
Rule Name | Value | Description
CONT.SE.3 | 0.12um | Minimum gate Contact to Active Area spacing
0.12um
0.12um
✄
Substrate
STI
ILD
POLY / Gate
CONTACTt
Gate-Active Short 방지를 위한 최소 Gate Contact 간격

## Slide 10: Why Contact-to-Gate Spacing Matters
Hot Carrier Injection Reliability
Pinch-off

## Slide 11: HCI(Hot Carrier Injection)
Charge trap formation
Device Degradation
Impact ionization rate :
Reliability Issue

## Slide 12
Substrate
Cadence Reproducing and vertical structure
Cadence
Schematic in Design Rule Manual
Rule Name | Value | Description
CONT.E.4 | 0.06um | Minimum N+/P+ Implant on Active Area to Contact enclosure
0.06um
0.06um
0.06um
0.06um
✄
P+
CONTACT
Sillicide
OXIDE
OXIDE
0.06um
Substrate
CONTACT
Sillicide
OXIDE
OXIDE
0.06um
N+
안정적인 Ohmic Contact 형성 및 Contact 저항 감소를 위한 Implant Enclosure 규정

## Slide 13
이상적인 경우, 형성되는 barrier height는 Schottky-Mott Rule에 의해 금속의 Work Function과 반도체의 Electron Affinity로 결정
Schottky contact (p, n type)
Metal과 semiconductor는 각각 다른 work function을 가짐. (서로 다른 Fermi level)
접촉 후 Fermi level을 일치시키기 위해 전자가 이동, semiconductor의 Band가 휘어지며(Band Bending) Schottky Barrier가 형성.
(NMOS)

## Slide 14
실제 CMOS에서는 Bardeen model에 의해 Fermi level이 pinning되어 work function 조합만으로 contact 특성이 결정되지 않음.
Ideal
Reality

## Slide 16
Schrödinger Equation :
Time independent and 1D :
,
Doping() | W() | T
 | 26.6 | 
 | 1.19 | 
 | 0.84 | 
 |  | T
 | 26.6 | 
 | 1.19 | 
 | 0.84 | 

## Slide 17
Cadence Reproducing and vertical structure
Cadence
Schematic in Design Rule Manual
Rule Name | Value | Description
CONT.SE.5 | 0.24um | Minimum Poly Contact to non-salacided Poly resistor or Active Contact to non-salacided Active resistor spacing
0.24um
0.24um
✄
Substrate
STI
CONTACTt
POLY / Gate
Silicide
저항 특성 유지 및 Salicide 침범 방지를 위한 최소 Contact-Resistor 간격 규정

## Slide 18: Why Non-salicided Resistor
Salicide : ultra-thin film->sheet resistance highly sensitive to thickness -> poor reproducibility
Non-salicided : -> determined mainly by implant dose
Poly / active (implant)
Salicide block mask
Salicide (junction)
thin, sensitive → low reproducibility
Salicide (junction)
thin, sensitive → low reproducibility
Non-salicided resistor body
R_sh set by implant dose → precise

## Slide 19: Non-salicide Boundary
Transfer length :
즉, Contact이 너무 가까우면 유효 폭 확보가 불가해 길이가 왜곡된다.
Salicide (low R)
Non-salicide resistor (high R)
Contact

## Slide 20: Salicide encroachment risk
Salicide block mask overlay error
Effective non-silicide resistor length becomes shorter than designed
Designed non-salicide length
Encroachment

## Slide 21
Cadence Reproducing and vertical structure
Cadence
Schematic in Design Rule Manual
Rule Name | Value | Description
CONT.X.1 | - | Contact on gate is NOT allowed
✄
Substrate
Active 위에 있는 Gate Poly(채널 영역) 위에는 Contact를 놓으면 안 된다
Active area
P+
STI
POLY / Gate

## Slide 22: Contact causes field crowding at the edge
Contact behaves as an equipotential body
Contact close to / overlapping the gate edge → vertical E-field locally enhanced at that point
Contact (equipotential)
Gate
Active area
Gate edge
Field lines crowd toward the gate edge

## Slide 23: Reliability risk ① : TDDB acceleration
(γ = field acceleration factor)
Field crowding → locally higher at the gate edge → drops sharply there → early breakdown risk
Chart: t_BD vs E_ox (E-model, schematic)
| E1 | E2 | E3 | E4 | E5 | E6
t_BD | 95 | 70 | 45 | 24 | 10 | 3
Local hotspot under contact → shifted to high-E_ox, low-t_BD region

## Slide 24: Reliability risk ② : direct tunneling leakage
Thin gate oxide (≲ 3 nm): electrons tunnel through the full barrier thickness (direct tunneling)
Local field enhancement → tunneling probability spikes → excess gate leakage at that spot
Barrier (gate oxide)
Si substrate
Locally thinner barrier under the gate edge → tunneling probability T ↑ sharply

## Slide 25: Metal

## Slide 26
Cadence Reproducing and vertical structure
Cadence
Schematic in Design Rule Manual
Rule Name | Value | Description
METAL1.W.1 | 0.12um | Minimum Metal 1 width
0.12um
✄
0.12um
Substrate
Silicide
OXIDE
CONTACTt
ILD
METAL 1
N+
공정 안정성 및 배선 신뢰성 확보를 위한 최소 Metal1 폭 규정

## Slide 27
Cadence Reproducing and vertical structure
Cadence
Schematic in Design Rule Manual
Rule Name | Value | Description
METAL1.A.1 | 0.07 | Minimun bent Metal1 area
Rule Name | Value | Description
METAL1.A.1 |  | Minimun bent Metal1 area
0.07
✄
Substrate
ILD
STI
공정 안정성 및 배선 신뢰성 확보를 위한 최소 Metal1 면적 규정
0.59um
0.12um

## Slide 28: Electromigration

## Slide 29: Quantifying Lifetime
Mean Time To Failure
: activation energy
n : current density exponent
J : MTTF decreases
T : MTTF also decreases
Chart: MTTF vs J (schematic)
| J1 | J2 | J3 | J4 | J5 | J6
MTTF | 95 | 68 | 42 | 22 | 9 | 3
Narrower Metal1 → higher J → shifted to the low-MTTF region

## Slide 30
감사합니다